Elastic anisotropy of bone

Biomechanics, BME 315

Tensorial elastic moduli (GPa), determined ultrasonically

Fresh bovine phalanx (2.2.9)                            Dry human femur (2.2.10)

C1111	19.7			23.4

C1122	12.1			9.06

C1133	12.6			9.11

C3333	32.0			32.5

C2323	5.4			8.71

Elastic anisotropy of bone. Technical elastic moduli. Wet human femoral bone by mechanical testing (2.2.2)  and bovine femoral bone by ultrasound (2.2.11).

Young's moduli (GPa)                    	Shear moduli(GPa)      	Poisson's ratios

(dimensionless)

Human	Bovine	         Human	Bovine                 Human	Bovine

Elong   	17       	22	Glong     3.6  	5.3	ν    0.58	0.30

Etransv    	11.5  	15	Gtr         3.3  	6.3	ν    0.31	0.11

Etransv    	11.5  	12	Gtr        3.3  	7.0	ν    0.31	0.21

The stiffness of compact bone tissue depends on the bone from which it is taken. Fibular bone has a Young's modulus about 18% greater, and tibial bone about 7% greater, than that of femoral bone. The differences are associated with differences in the histology of the bone tissue. Bone is elastically anisotropic, i.e. its properties depend on direction. Such behavior is unlike that of steel, aluminum and most plastics, but is similar to that of wood.

Strength	Density

Material                      	σult[MPa]	ρ(g/cm3)	σult /ρ

polyethylene (high density) 	20-40	0.95	21-42

polymethyl methacrylate (PMMA)	70	1.18  	59.3

human compact bone

longitudinal	148	2.0   	74	.

transverse	 	49

steel (structural)	400	7.8	51.3

aluminum (1100-H14)	110	2.71	40.6

granite	 	20	2.77	7.2

concrete (compression)	28	2.32	12.1

modulus	Density

Material                      	E[GPa]	ρ(g/cm3)	E/ρ	E/ρ2

polyethylene (high density) 	0.5	0.95	0.53	0.55

polymethyl methacrylate [PMMA]	3.0	1.18  	2.5	2.15

human compact bone

longitudinal	17	1.8   	9.4	5.2

Dentin	13-18

Enamel	50-84

steel(structural)	200	7.86	25.4	3.23

aluminum	70	2.71	25.8	9.53

concrete	25	2.32	10.8	4.6

wood(pine)	11	0.61	18.0	29.6

References

2.2.2	Reilly, D.T. and Burstein, A. H., The elastic and ultimate properties of compact bone tissue,  J. Biomechanics, 8, 393-405, 1975.

2.2.9	Lang, S.B., Ultrasonic method for measuring elastic coefficients of bone and results on fresh and dried bovine bones, IEEE Trans. Biomed. Eng., BME-17, 101-105, 1970.

2.2.10	Yoon, H.S. and Katz, J. L., Ultrasonic wave propagation in human cortical bone. II Measurements of elastic properties and microhardness, J. Biomechanics, 9, 459-464, 1976.

2.2.11	Van Buskirk, W. C. and Ashman, R. B., The elastic moduli of bone, in Mechanical Properties of Bone, Joint ASME-ASCE Applied Mechanics, Fluids Engineering and Bioengineering Conference, Boulder, CO, 1981.